## Slide 1
SSPC Standards Update March 2019
NSRP SP&C Panel, March 12-14 2019 Charleston, SC
John Kern
SSPC Technical Services Dept.

## Slide 2: Topics
Ongoing Revision Projects 2019 Update
  SSPC-SP 11, Power Tool Cleaning to Bare Metal; and SSPC-SP 15, Commercial Grade Power Tool Cleaning
  SSPC-PA 17, Procedure for Determining Conformance to Steel Profile/Surface/Roughness/Peak Count Requirements
  Proposed revisions to SSPC/NACE Joint Dry Blast Cleaning Standards
  QP 2 Standard Revision (QP 1 revision is complete)

## Slide 3: Topics (cont’d.)
New Projects
  Standard for Thorough Blast Cleaning of Non-Ferrous Metals
  Possible standard for surface cleanliness using non-profiling surface preparation techniques (plasma blast, laser ablation, possibly dry ice) that do not generate secondary waste stream

## Slide 4: 2019 Revisions – SP 11 and 15
No significant change in cleanliness requirements
Proposed table for selection of tool types for various uses, e.g.
  Rust removal
  Removal of single coating layer
  Removal of all coating layers
  Creation of anchor profile
  Feathering edges

## Slide 5: Proposed Revisions SP 11 and 15
Addition of a tool selection table is proposed
Table will describe various existing conditions and the appropriate tools to use for best results on each condition
Tentative plans for demo of various tool capabilities at SSPC 2020 conference
Proposal for new cleanliness standard submitted by MontiPower, but needs more “grassroots support” from users and contractors to be developed as a separate standard

## Slide 6: Power Tool Selection Table
Still a “work in progress”
Types of tools (still in discussion) include
  Grinding wheels
  Coated abrasive discs/belts/flaps
  Nonwoven abrasive flap
  Nonmetallic brush
  Metallic brush
  Rotary flapper
  Cutter bundle
  Bristle impact
  Needle gun

## Slide 7: SP 11 on Ship Deck

## Slide 8: Revision PA 17 (Compliance to Profile Requirements)
New appendix that describes techniques for measuring profile on severely pitted substrates
  Take readings on non-pitted area of substrate if available
  Create companion coupon of non-pitted steel to evaluate profile created by the abrasive
Definitions are being revised to reflect revisions in ASTM D4417 - waiting for publication of revised D4417 before continuing work

## Slide 9: Heavily Pitted Steel

## Slide 10: 2019 Revision of SSPC-PA 2
Revision issued January 2019
Added nonmandatory appendix describing use of scanning probe technology to acquire readings

## Slide 11: Scanning Probe

## Slide 12: PA 2 Appendix 10 Highlights
Scanning Batch Measurement – mean of no fewer than 12 and up to 24 DFT readings w/o lifting probe from coated surface
  Readings taken within 645 m2 (~100 in2) segment of coated area
Scanning Area Measurement – sample mean of 5 scanning batch measurements obtained over each 10 m2 (~100 ft2)

## Slide 13
Large box represents 100 ft2 area (scanning area)
Smaller boxes represent 100 in2 areas (scanning batch)

## Slide 14: Revisions to Joint Dry Blast Standards
First ballot issued mid-February 2019, responses due March 24
Committees voting on “template” language revisions that affect all five dry blast standards
SSPC-SP 10/NACE No. 2 has been chosen to provide the “template”
Most changes proposed to reflect parallel language in joint WAB standards issued in 2018

## Slide 15: Revisions to Dry Blast Standards
Propose to add
  Info on removal of pack, stratified, rust scale as in 2018 revisions of SP 2 and SP 3 (include instructions for methods and extent of removal in project spec)
  Nonmandatory commentary sections on nonvisible contaminants, definition of staining, example of specification statement
No plan to change the existing cleanliness definitions

## Slide 17: Standard for Thorough Blast Cleaning of Non-Ferrous Metals
Cleaning of previously coated non-ferrous alloys (copper, aluminum), stainless steel for subsequent coating application
Organization similar to dry blast cleaning standards for steel
Non-mandatory appendices contain supplementary info on selection of abrasives, blast pressures, chemical cleaning, profile, etc.
Draft has had one ballot, discussion of use of “staining” vs. ”color variation” is ongoing.
Pete Ault may provide additional details

## Slide 18: Possible Non-Profiling SP Standard
Might include use of laser ablation, dry plasma blasting, and possibly dry ice blasting??
Proposal requires SSPC Standards Review Committee approval after scope and methods are more defined – needs industry cooperation from all technologies
Matt Binsfield will provide update on status

## Slide 19: QP 1 2019 Revision
Revised standard issued January 7, 2019
Audit Checklist not yet updated to reflect revisions
No audits to the 2019 requirements are planned until 2020
Clarifications to subcontracting requirements and requirements for EH&S manager training and education are the principal changes

## Slide 20: QP 2 Revision
Still in consensus committee review
Ballot of Draft #3 expected in April
Subcontracting and EH&S revisions will parallel those in revised QP 1
Revisions to Audit Checklist will start after standard is approved and require approval by PCCP Advisory Committee

## Slide 21
THANK YOU!
Questions?