## Slide 1: Additive Manufacturing Qualification, Certification and Implementation
Dongchun, Mary, Qiao and Demetri Stroubakis
American Bureau of Shipping (ABS)
Oct 16, 2019

## Slide 2: Outline
Background
Benefits
Additive Manufacturing Processes
Qualification
Certification
Implementation
Summary

## Slide 3: Background
Traditional Manufacturing
  Materials Manufacturing
    Rolling, Casting, Forging etc.
    To meet mechanical properties by Heat Treatment etc.
  Machining
    To meet dimension and special features by CNC machine, Lathe etc
  Welding
    To join multi-pieces together
Additive Manufacturing
  Integrated process with materials manufacturing machining and welding
  Add materials layer by layer
  Controlled by sliced CAD model, software and hardware

## Slide 4: Benefits
Digital Scanning
Digital Design
Digital Engineering
Digital Manufacturing
Manufacturing On-Demand
Prototype new design
Reduce inventory of spare parts
Remanufacture obsolete parts
Reduce lead-time
Repair or Special Feature
Apply functional/new materials
Add specific features
Repair damaged parts
Manufacturing End Use Components
Increase design freedom for complex shapes
Integrate multiple pieces to single part
Add materials for weight saving
Small Batch Production
Cost-effective small volume production
Small batch production under dynamic vs static build

## Slide 5: Additive Manufacturing Processes
Objectives of ABS are Qualification of AM Facilities to enable reliable quality products through a developed certification scheme which focuses on:
  Design verification and validation
  Additive manufacturing procedure approval
  Initial and periodic factory audits

## Slide 6: Additive Manufacturing Processes
ASTM F42
Categories of Additive Manufacturing Processes
Materials Extrusion
Material Jetting
Vat Photopolymerization
Sheet Lamination
Binder Jetting
Direct Energy Deposition
Powder Bed Fusion

## Slide 7: Powder Bed Fusion Example
Powder Bed Fusion (PBF): An AM process in which thermal energy selectively fuses regions of a powder bed.
Example of Build Diagram Showing Location, Number, Type, and Orientation of Test Specimens and Reference Parts
Distance Between Parts
Nesting
Type and Arrangement of Part and Support Structures
Powder Roller
Powder Supply
Build Platform / Baseplate
Powder Matrix
Energy Source & Beam Controller

## Slide 8: Directed Energy Deposition Example
Direct Energy Deposition (DED): An AM process in which focused thermal energy is used to fuse materials by melting as they are being deposited.
X
Y
Z
Process Coordinate System
Multi-Axis Arm
Maximum Working Envelope / Build Volume
Deposition Path
(Contour or Fill Types, Contour Shown)
Build Platform or Existing Part
Part Fixture
(Can be Static or Dynamic)

## Slide 9: Binder Jetting Examples
Binder Jetting (BJ): An AM process in which liquid bonding agent is selectively deposited to join powder materials
Powder Spreader and / or Inkjet
Loose Powder
Bound Powder
Build Box
Direct Metal Production
Indirect Metal Production
To Infiltration & Heat Treatment
Bound Metal Powder Parts
Bound Sand Mold
To Casting Facility
Bound Part Cores
(if applicable)

## Slide 10: Additive Manufacturing Processes
AWS D20.1
Subcategories of Metal Additive Manufacturing Processes | Abbreviation
Laser Powder Bed Fusion | L-PBF
Electron Beam Powder Bed Fusion | EB-PBF
Laser Directed Energy Deposition | L-DED
Electron Beam Directed Energy Deposition | EB-DED
Plasma Arc Directed Energy Deposition | PA-DED
Gas Tungsten Arc Directed Energy Deposition | GTA-DED
Gas Metal Arc Directed Energy Deposition | GMA-DED

## Slide 11: Qualification
Critical/Severity level for application may be determined and agreed. Appropriate AM process is selected and routing out.
June 2016, International Journal of Fatigue 94,
DOI: 10.1016/j.ijfatigue.2016.07.005 Michael Gorelik, Federal Aviation Administration
Critical:
  Failure would cause significant danger to personnel, loss of control, loss of a system, loss of a major component or an operating penalty.
Semi-critical
  Failure would reduce the overall strength of the equipment or system or preclude the intended functioning or use of equipment, but loss of the system or the endanger of personnel would not occur.
Non-critical
  Failure would not affect the operation of the system or endanger personnel.
AWS D20.1

## Slide 12: Qualification
Feedstock
(Powder/Wire)
Part/Coupon Design
(CAD files, functional and technical design specs)
Additive Manufacturing Service Provider
Production Parts
Reference Parts
Test Samples
Test Artifacts
Heat Treatment
(AM processes can build significant residual stresses)
Cleaning/Machining
(Not trivial if complex geometry)
Testing
Destructive
Nondestructive
Functional
Application
Partial Black Box
Machine operations are observed, but data may not be well-understood or shareable.

## Slide 13: Qualification
Additive Manufacturing Qualification Process
Cradle to Grave File
Part Design Package
Part Inspection and Testing Package
Part Manufacturing Description
Process Configuration and Workflow Diagram
Additive Manufacturing Project Setup
Initial Cradle to Grave File Population
Feasibility Stage
Verification Stage
Pre-Production Validation Stage
Production Stage
Qualification Stages

## Slide 14: Qualification
Sample Additive Manufacturing Qualification Record: Machine Qualification or Procedure Qualification Record:
  General
  Build Platform
  Feedstock
  Machine
  Environment
  Build Parameters
  Post Processing
  Examination and Testing Results (additional testing by design requirements)
  Refer to AWS D20.1

## Slide 15: Qualification
Challenges
  Process-Microstructure-Properties
  Mechanical properties (anisotropy, fracture toughness, fatigue properties etc.)
  Process-Feature-Function
  Non-destructive testing
  Verification and validation in manufacturability, maintainability and reliability
http://senvol.com/database/

## Slide 16: Qualification
Fit-For-Service
  Severity zone based
  Engineering Critical Assessment
    BS 7910
    Crackwise developed by the welding institute, UK
  Risk based
    Statistics data of traditional manufacturing vs additive manufacturing
Chart: Initial Flaw Length, 2C, mm
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 15 | 15 | 17 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60
CTOD | 30 | 25 | 24 | 20
Non-CTOD | 6 | 5 | 4 | 3

## Slide 17: Certification
Metal Additive Manufacturing Component
  Product Design Assessment
  Manufacturing Assessment
  Product Quality Assessment
  Unit Certification
Additive Manufacturing Service Provider
  Quality Management System
  Additive Manufacturing Capability
Request for Approval
Instruction Letter
Submittal Review
Audit
Maturity Letter or Provisional Approval Letter
Capability Demo.
Approval Letter or Certificate

## Slide 18: Implementation
Additive manufacturing process is continuously improved using a close-loop product lifecycle management.
Approved Design
Approved Raw Material Supplier
Outsourcing Suppliers
Approved AM
Machine Procedure Operator
Approved Production Plan
Accepted Inspection and Testing Report
Traceable during Operation
Performance Evaluation or Failure Analysis

## Slide 19: Summary
  Metal AM for end-use can bring many benefits for shipping industry.
  Manufacturing on-demand
  End-use components
  Repair or add features
  Small batch production
  Three common metal AM processes:
  PBF
  DED
  Binder Jetting
  NTQ for other processes requested
  ABS streamlined qualification scheme, certification and implementation process.
  Additive Manufacturing Service Provider
  Metal Additive Manufacturing Components

## Slide 20: Summary
  ABS Advisory
  https://ww2.eagle.org/content/dam/eagle/advisories-and-debriefs/ABS_Additive_Manufacturing_Advisory_17294.pdf
  ABS Guidance Notes
  https://ww2.eagle.org/content/dam/eagle/rules-and-guides/current/other/299-gn-on-additive-manufacturing-2018/additive-manufacturing-gn-sept18.pdf
  ABS Steel Vessel Rules
  https://ww2.eagle.org/en/rules-and-resources/rules-and-guides.html
  ABS Current Engagement
  Joint Development/Industry Project to improve the technology readiness level of additive manufacturing technology for marine and offshore application.